|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| |  | | --- | |  | | **Track Shoes**  http://www.bercoamerica.com/images/products/misc.jpg  **Widest selection of track shoes for every application**   • Over 50 different profiles of Single, Double and Triple grouser shoes  • Many different shoe configurations such as width, chamfered holes, mud holes, and clipped corners  • Cast steel shoes: Self-cleaning (swamp type) to be used in sticky type soils and flat type for running on concrete or hard surfaces  • Forged shoes for special applications like mining  • Rubberized, polyurethane and rubber clamped-on steel shoes, typically used on paving machines  • Over 4,000 different shoes, to match any chain or application  • Shoes for machines with a chain pitch ranging 3.97” – 13.78” (100 – 350mm)   |  |  |  | | --- | --- | --- | |  |  |  | | Track Shoe | Track Shoe | Track Shoe | | **Single Grouser Shoes** Typically for dozers when grip and traction are the main factors. **Chain Pitch 4.9" -- 12.5"** | **Double Grouser Shoes** Typically for loaders when medium traction and maximum maneuverability are needed.  **Chain Pitch 4.0” -- 11.3”** | **Triple Grouser Shoes** Typically for excavators, when a firm grip, low ground pressure and maneuverability are needed. **Chain Pitch 4.9” – 9.0”** |   **Your Best Undercarriage Value**  Berco Track Shoes are through hardened and stress relieved to guarantee excellent wear, high strength and resistance to bending and breakage resulting in longer shoe life.  **The Process and Materials**  • Heavy duty rolled steel profiles  • Low alloyed Boron Steels with certified hardenability based on Berco specification  • Surface hardness HRC 47 for reduced wear and longer life  • Precise designs carefully manufactured for proper fit   |  |  |  | | --- | --- | --- | | Track Shoe | Track Shoe | Track Shoe | | |  | | --- | |  | |
|  | |